INTEROFFICE COMMUNICATION

TO: David James P.E., District Contracts Manager

FROM: Nicholas Chaney, P.E., District Bridge Engineer

DATE: June 25, 2026

SUBJECT: Abbreviated Structure Type Study (STS) for bridge MAH-170-08.03 (SFN: 5004020) PID:123676

This memo serves as an abbreviated structure type study for the subject bridge to assist in establishing a rehabilitation or replacement strategy. The conclusions of this study are based upon analysis of the existing structure design, previous project history, existing conditions, and field observations.

Existing Structure Overview

MAH-170-08.03 is a 110’-5” long, 44’ wide, three-span continuous reinforced concrete slab bridge carrying SR 170 over Burgess Lake in Poland Township. The bridge was constructed in 1959 and consists of a 15" concrete slab superstructure supported by HP12x53 capped-pile piers and pile-supported abutments. The structure is set on a 30-degree skew.

Past rehabilitation work includes deck-edge replacement (2014), a 3 ¼" concrete overlay (2020), and pile encasement with minor substructure patching (2021). The most recent load rating indicates the bridge currently supports 137% of the legal load for H20 design loading.

Condition Assessment

The 2025 bridge inspection rates the structure general appraisal as fair (5 rating). This rating is driven by fair (5) superstructure and deck conditions. Deficiencies are primarily seen in the deck underside including widespread saturation, moderate to significant efflorescence, delaminations, and longitudinal cracking through all spans. Rust staining is present in previously repaired areas, suggesting ongoing deterioration of reinforcing steel. The wearing surface exhibits minor cracking in both lanes, with moderate map cracking above both piers.

The substructure (rated 6) is in satisfactory condition. Deterioration is present in prior abutment repairs and in isolated delaminated areas along the abutment/deck interface. The exposed portion of the steel piles show varying degrees of corrosion with section loss noted at the top of piles 5 and 6 of pier 1.

Findings

Given the extent of deck saturation, efflorescence buildup, rust staining, and delamination in the deck floor, and the structure's overall age, a superstructure replacement is warranted. Minor rehabilitation measures, such as installing a new concrete overlay, are not economically viable since subsequent overlays offer no significant extension of service life without excessive full depth patching. The satisfactory condition of the substructure (rated 6) indicates a full structure replacement is unnecessary per BDM C401.4. Nonetheless, minor repairs to the existing substructure will be required.

Design Alternatives

For all alternatives, existing substructure elements would be re-used as much as possible with some modification to both the roadway profile and substructure to accommodate a thicker superstructure profile over the existing 15” slab depth. The proposed structure’s low‑chord elevation should match the existing elevation to maintain the hydraulic opening. Three superstructure replacement alternatives have been investigated:

Concrete Slab Superstructure

This alternative replaces the superstructure in kind with a presumed 21” depth concrete slab deck.

PROS:

- Maintains the existing load path, minimizing required substructure analysis or modifications.

- Longest service life of all alternatives considered.

CONS:

- Longer construction duration and higher initial cost (without considering substructure modification).

- Longer roadway closure

- The thicker slab deck would increase dead load by about 37%. The use of light weight concrete will be required to bring the dead load increase to approximately 14%

Prestressed Concrete Box Beam (PSBB) Superstructure with Composite Deck

This alternative involves replacing with a presumed 17” depth PSBB superstructure with an 8” composite deck (6” minimum + 2” sacrificial haunch). A Non-composite PSBB superstructure will not be considered due to insufficient service life.

PROS:

- Faster time to construct than in-kind slab replacement.

- Likely lowest initial cost (without considering substructure or roadway modification).

CONS:

- Requires substructure analysis and modifications due to the changed load configuration.

- Likely requires additional modification to the roadway profile compared to in-kind slab replacement.

- Likely shortest service life of all alternatives considered.

Steel Beam Superstructure

This strategy proposes a steel beam superstructure with or without a composite deck and would include a galvanized or metalized protection coating system (PCS).

PROS:

- Faster time to construct than in-kind slab replacement.

- Lower initial cost (without considering substructure or roadway modification).

- Good service life available if PCS is maintained

CONS:

- Requires substructure analysis and modifications due to the changed load configuration.

- Likely requires further modification to the roadway profile compared to in-kind slab replacement.

- PCS maintenance required.

Preferred Alternative

Due to the substructure analysis and modifications required for PSBB and steel options, an in‑kind replacement using a continuous reinforced concrete slab is the preferred alternative.

Design Considerations

- A new 21” slab with light weight concrete (125pcf) shows a dead load increase over the existing slab by approximately 14% which is permissible per BDM C401.4B. The dead load check did not account for the existing overlay and only compared original construction to the new proposed slab.

- To account for the new slab thickness, profile adjustments to SR 170 is anticipated to maintain the low chord elevation of the structure.

- If excavation behind the existing abutments is minimal, a design with shorter or no approach slab may be considered.

- The gas utility attached to the right side of the structure will be relocated off the bridge.

- All substructure elements shall be re-used with modification expected to the top portions of the abutments and pier caps along with any minor repairs. The designer should consider incorporating galvanic anodes in repaired portions of the substructure to extend service life.

MOT Considerations

The district’s preference is to close and detour SR 170 for the duration of the project. Access to Hummingbird and Thunderbird Dr will shall be maintained at all times.

Conclusion

The recommended rehabilitation strategy for MAH-170-0803 is an in‑kind superstructure replacement using a concrete slab deck with lightweight concrete (125 pcf) to limit dead‑load increase. The design shall maintain the existing low chord elevation and adjust roadway profile to accommodate the thicker slab.  A planning level estimate for the above scope of work is $1.75 million. Further refinement of the cost estimate is anticipated upon the completion of conceptual / stage 1 review.