STATE OF OHIO DEPARTMENT OF TRANSPORTATION

BRIDGE INSPECTION REPORT

| BR-86 REV 2-95 |  |
| --- | --- |
| 1 | 8 | 0 | 5 | 4 | 3 | 6 | BRIDGE NUMBER | CUY | 00176 | 1334 | CUYAHOGA | YEAR BUILT | 1968 |
| STRUCTURE FILE NUMBER 7 | CO | ROUTE | UNIT |  |
| DIST | 12 | BRIDGE TYPE | 322 | TYPE SERVICE | 10 |  | IR-71 NB (CUY-71-1791R) |

For Full Report, Please See Bridge File.  Curbs, Sidewalks, & Walkways do not exist so this item was removed.

DECK	FLOOR:  The floor is in fair condition.  There are hairline to narrow transverse cracks with efflorescence.  A few areas show honeycombing and spalling with exposed rebar.  There also are areas of delaminated concrete.

WEARING SURFACE:  The wearing surface is in fair condition.  There are areas of full-depth patches that are in good quality.  There are transverse cracks spaced roughly at 10 ft intervals in the positive moment regions and at 6 ft intervals in the negative moment regions.  There are isolated areas of map cracking, spalling, and deteriorated patches.  Several RPMs are missing leaving shallow holes.

RAILING:  The railing is in fair condition.  There are several spalls along the toe of the barrier.  Vertical cracks exist throughout.  There are longitudinal cracks with efflorescence on the exterior face in Span 19BE.  The spalling and cracking in the railing is the reason for lowering the rating to a 2, per the 2010 revision of the ODOT Manual of Bridge Inspection.

DRAINAGE:  The drains are in fair condition.  Several drains are clogged.  The rating was raised to a 2 since the amount of scuppers clogged is up to ¼, per the 2010 revision of the ODOT Manual of Bridge Inspection.

EXPANSION JOINTS:  The expansion joints are in fair condition.  The glands show signs of minor leakage.  Debris exists in most of the joints.  The elastomeric seal joint near Piers 13 & 24BE have a portion of the sealer sticking up out of the joint with tears in the sealer visible.  The elastomeric seal joint at Pier 24BE also have a ¼” to ½” elevated lip from one side of the joint to the other.  The elastomeric seal joint near Pier 18BE has portions of the armor missing.

SUPERSTRUCTURE	BEAMS/GIRDERS:  The beams and girders are in good condition.  There is surface corrosion at various locations, especially on the bottom flange, splice bolts, and near the seated hinges.  The area near the seated hinges has up to 1/16” section loss.  A loose bolt exists at the splice at Beam C, Span 18BW.

DIAPHRAGMS OR CROSSFRAMES:  The crossframes are in fair condition.  There are locations of corrosion holes in Spans 18BW and 13.  A paint crack exists in Span 15 on Beam L.  There is an incomplete weld in Beam A, Span 15.  Pack rust is bowing the top gusset plate 1” in Span 18BW.

BEARING DEVICES:  The bearings are in fair condition.  There are six bearings that are rocked ≥10°.  One bearing is rocked beyond recall; North Abut BE, Bearing G.

PAINT:  The paint is in satisfactory condition.  There is greater than 5% and less than 10% of the total coating system has failed.  Surface or freckled rust is prevalent throughout.  There are random locations of peeling paint and surface corrosion.

PINS/HANGERS/HINGES:  The seated hinges are in fair condition.  The hinges have surface corrosion with the corrosion heavier at the groove.

FATIGUE PRONE CONNECTIONS:  The fatigue prone connections are in good condition.  There is surface corrosion on the welds.

LIVE LOAD RESPONSE:  The live load response is in satisfactory condition.

SUBSTRUCTURE	ABUTMENTS:  The abutments are in good condition.  There is rust staining and map cracking.  This is the reason for raising the rating to a 1.  The previous deficiency noted is actually located on the backwall and that rating correlates with the problem.

PIERS:  The piers are in fair condition.  There are hairline to medium cracks, spalling with exposed rebar, and delaminations.

PIER SEATS:  The pier seats are in good condition.  There are multiple areas along the pier seat edge that are cracking.

BACKWALLS:  The backwalls are in fair condition.  There is map cracking at North Abut BW.

SLOPE PROTECTION:  The slope protection is in good condition.  The stone slope protection shows signs of erosion.

APPROACHES	PAVEMENT:  The pavement is in good condition.  There are spalls and patches in the asphalt adjacent to the expansion joints.

GUARDRAIL:  The guardrail is in good condition.  The impact attenuator between Pier 17 and Pier 18BW has been hit by a vehicle.

GENERAL	WARNING SIGNS:  There are no bridge end markers.

SIGN SUPPORTS:  The rating was raised to a 1 because there were no significant deficiencies noted.

VERTICAL CLEARANCE:  The rating was changed to a 1 since there is a restriction for traffic on the bridge and there are no changes from last year.