# 1st HALF 2026 Concrete Specifications

# For January 16, 2026 SS800 Posting

For the 2023 C&MS – Provide the following updates:

455.02

On Page 292 in 455.02 A. 5. ADD after the 3rd sentence the following:

When testing Self Consolidating Concrete, use ACI certified Self-Consolidating Concrete Testing Technicians.

499.03

On Page 304, Replace TABLE 499.03-1 with the following:

TABLE 499.03-1 CONCRETE MIX DESIGN REQUIREMENTS

| Quantities per Cubic Yard (Cubic Meter) Provide Concrete with 7±2% Air Content |  |  |  |  |
| --- | --- | --- | --- | --- |
| Class | Design Strength psi (MPa) | Permeability [1] Maximum (Coulombs) | Surface Resistivity [2] Minimum (kΩ-cm, α = 1.5) | Aggregate Requirements |
| QC 1 | 4,000 (28.0) at 28 days | 2,000 | 21 | Well-Graded |
| QC 1P[8] [9] | 4,000 (28.0) at 28 days | 2,000 | 21 | Well-Graded |
| QC 2 | 4,500 (31.0) at 28 days | 1,500 | 29 | Well-Graded |
| QC 3 Special | As per plan | 1,500 or as per plan | 29 or as per plan | Well-Graded or as per plan |
| QC 4 Mass Concrete [4] [5] | 4,000 (28.0) or as per plan [3] | 2,000 or as per plan | 21 or as per plan | Well-Graded or as per plan |
| QC 5 [7] | 4500 (31.0) at 28 days | N/A | N/A | 1 inch or 3/8-inch nominal maximum size |
| QC SCC [7] | 4500 (31.0) at 28 days | 1,500 or as per plan | 29 or as per plan | Well-Graded, 1 inch or 3/8-inch nominal size or as per plan |
| QC MS | See Supplement 1126 | N/A | N/A | 1-inch nominal maximum size |
| QC RS[10] | See Supplement 1126 | 2,000 | 21 | Well-Graded |
| QC Misc. [6] | 4,000 (28.0) at 28 days | N/A | N/A | 1-inch nominal maximum size |
| [1] AASHTO T277 Modified. Mix design must meet either permeability or resistivity requirement. [2] AASHTO T358 Modified. Mix design must meet either permeability or resistivity requirement. [3] Strength for Mass Concrete (QC 4) may be tested at either 28 or 56 days. [4] Do not use Type III cement or accelerating admixtures in mass concrete. [5] The maximum fly ash, natural pozzolan, or slag cement content may be increased up to 50%. [6] For QC Misc. mixes only –Water/Cementitious ratio limited to 0.50 maximum. [7] For QC 5 and QC SCC mixes with 3/8-inch nominal size, provide an air content of 8±2%. [8] Portland cement concrete pavement mix design. [9] QC 1P may be used in lieu of QC 1. QC 1 may not be used in lieu of QC 1P. [10] Provide QC RS with 6±2% air content. |  |  |  |  |

On Page 304, ADD the following sentences between the last 2 paragraphs on the page:

Determine the resistivity by testing according to AASHTO T358 except test 4” x 8” cylinders cured in lime-water. Perform resistivity testing at 28 days.

For 2023 C&MS

Supplement 1126 Developing and Submitting a Portland Cement Concrete Mix Design for Approval

SCD BP-2.2 Transverse Pavement Joints

SCD BP-2.3 Pressure Relief Joint Type A

SCD BP-2.5 Rigid Replacement