STATE OF OHIO

DEPARTMENT OF TRANSPORTATION

Supplimental Specification 800

revisions to the 2023 CONSTRUCTION & MATERIAL SPECIFICATIONS

Dated  01-16-2026

SS800 Publication

Item 611

On page 498, Replace the entire section H. with the following language:

H.	For bedding and backfill, furnish materials conforming to:

Bedding……………….	703.11, 613.03 Type 2, 613.05 Alternative Mix

Structural Backfill ……703.11, 	613.03 Type 2, 613.05 Alternative Mix

Final Backfill:

Granular Structural Backfill 	703.11

Natural Soils  	703.16.A[1]

Granular Embankment

Materials 	703.16.B[1]

Granular Embankment Material

Types A, B, C and D	703.16.C[1]

Coarse aggregate	Table 703.01-1

Fine aggregate

703.02.A, 703.03, or 703.05.A

304	703.17.A

410, 411, and 617	703.18.A[1]

Low Strength Mortar

Backfill (LSM)	………….613.03 Type 2, 613.05 Alternative Mix

[1] Use any type of material defined as suitable materials for embankment construction except for steel slag, PCS and RAP.

On page 499, Remove the following paragraph from the page:

If a precast reinforced concrete 3-sided flat topped culvert (706.051), a reinforced concrete arch section (706.052), or a precast reinforced concrete round section (706.053) is specified, the Engineer may allow the Contractor to substitute one for the other. Refer to 611.04 for submittal requirements.

On page 504, Add the following sentences after the fifth sentence of second paragraph of Section 611.06 Bedding and Backfill:

Mix and place LSM per 613. Apply exterior coating to aluminum and aluminized steel conduits according to 611.09 C. prior to placement of LSM Bedding or Backfill.

On page 509, Add the following paragraph after the third paragraph from the top of the page:

C. Completely coat the outside of all aluminum or aluminized steel conduits (707.01, 707.02, 707.21, 707.22, 707.23, 707.24, 707.25) with a zinc chromate-free primer or an epoxy paint formulated for aluminum  when using LSM (613) for Bedding or Backfill.

On page 511, Replace the first sentence of the first full paragraph with the following sentence:

Completely coat the area to be paved with a zinc chromate-free primer or an epoxy paint formulated for aluminum on all aluminum or aluminized steel conduits (707.01, 707.02, 707.21, 707.22, 707.23, 707.24, 707.25).

On page 512, Replace the second row of the table in the first full paragraph from the top of the page with the following:

| Conduits with a rise of 36 inches (900mm) up to 60 inches (1524mm) | Manual or Remote inspection |
| --- | --- |

700 Section

707.12 Corrugated Steel Spiral Rib Conduits.

On page 797, Replace the next to last line of the table with the following language:

| 114 | 0.138 |  | 2850 | 3.51 |
| --- | --- | --- | --- | --- |