STATE OF OHIO DEPARTMENT OF TRANSPORTATION

SUPPLEMENT 1008

METHOD OF TEST FOR GLASS BEADS (740.09) and WET REFLECTIVE OPTICS (SS905)

January xx, 2026

| 1008.01 | Types |
| --- | --- |
| 1008.02 | Apparatus |
| 1008.03 | Sampling |
| 1008.04 | Sieve Analysis |
| 1008.05 | Calculations |
| 1008.06 | Roundness |
| 1008.07 | Coatings |
| 1008.08 | Refractive Index |
| 1008.09 1008.10 | Reflectivity Heavy Metals |

1008.01 Types.

- 740.09, Type A, paint glass beads

- 740.09, Type B, polyester glass beads

- 740.09, Type C, thermoplastic glass beads

- 740.09, Type D, epoxy glass beads

  - Size I: sieve nos. 10 through 20 (2.00 mm through 850 um)

  - Size II: sieve nos. 20 through 100 (850 m through 150 m)

- SS905, Wet Reflective Optics

# 1008.02 Apparatus.

- Analytical balance, accurate to 0.0004 oz. (.01 g)

- Sample splitters

  - 16-to-1

  - 1:1

- Mechanical shaker

- Roundometer

- Sieves:

  - 8 inch (200 mm), half- and full-height, stainless steel frame and mesh, sieve nos. 20, 30, 50 and 100 purchased and verified to ASTM E 11.

  - The remainder are 8 inch (200 mm), half- and full-height, stainless steel frame and mesh, purchased and verified to ASTM E 11.

- Computerized optical particle analyzer

- Microscope

- Drawn down bar

- Bead drop box

- Portable retroreflectometer

- X-Ray Fluorescence Spectrometer

- Handheld retroreflectomer

- Handheld colorimeter

# 1008.03 Sampling.

ASTM D 1214, Sieve Analysis of Glass Spheres, Section 6 and AASHTO R98 Determination of Size and Shape of Glass Beads Used in Traffic Markings by Means of Computerized Optical Method Section 11.1

- Paint, polyester, thermoplastic and epoxy size II beads. Obtain one representative sample of approximately 1 gallon (4 liters), or 1 quart (1 liter) by means of a 16 to 1 riffle sampler, from three bags, each from randomly selected racks, constituting a 44, 000 lb. (20,000 kg) shipment of 22 racks. From the 1 gallon (4 liter) or 1 quart (1 liter) sample, obtain an appropriate test sample by means of a sand splitter. Use the test sample on an as-received basis, unless noticeably damp.

- Epoxy size I beads and Wet Reflective Optics. Obtain one representative sample of approximately 1 gallon (4 liters), or 1 quart (1 liter) by means of a 16 to 1 riffle sampler, from two bags, each from randomly selected racks, for each 10,000 lbs. (4500 kg) shipment of five racks. From the 1 gallon (4 liter) or 1 quart (1 liter) sample, obtain an appropriate test sample by means of a sand splitter. Use the test sample on an as- received basis, unless noticeably damp.

# 1008.04 Sieve Analysis.

- Place the test sample on the top-most sieve of the stack and put the sieve stack in the mechanical shaker. Mechanically sieve for 15 minutes.

- Proceed as in ASTM D 1214, Section 7.1.3.

- Weigh and record the weight of the contents of each sieve to the nearest 0.0004 oz. (0.01 gram).

- Alternative testing method for sieve analysis is performed using computerized optical particle analyzer and AASHTO R98

# 1008.05 Calculations.

- Paint and polyester beads: calculate the total percent passing each sieve, expressed to the nearest 0.1 percent.

- Thermoplastic and epoxy sizes I and II: calculate the total percent retained for each sieve, expressed to the nearest 0.1 percent.

- Wet Reflective Optics: calculate percent passing or retained on each sieve according to manufacturer’s gradation

# 1008.06 Roundness.

ASTM D 1155, Procedure B, or the overall rounds results from the alternative testing method using computerized optical particle analyzer and AASHTO R98 shall be utilized to determine compliance.

- In all cases, final inspection of the rounds and unrounds by microscope will show 95+% separation if properly separated.

- If performing testing according to ASTM D 1155 the contents of each sieve from 1008.04 shall be used.

# Coatings.

1.	AASHTO T346 shall be used to determine compliance.

# 1008.08 Refractive Index.

- Tested by liquid immersion method, ASTM C1648 Becke Line Method or equivalent

# 1008.09 Reflectivity.

- Samples shall be tested according to ASTM D8367 utilizing ODOT approved binder materials and application rates.

- Alternative methods of test as specified by the manufacturer.

# 1008.10 Heavy Metals.

- AASHTO T392 shall be used for verification testing.