709.16	Galvanized Steel Reinforcement.   Provide galvanized steel reinforcement in accordance with ASTM A767, Class 1, 2 or ASTM A1094.

Galvanized steel reinforcement may be provided as an option to 709.00. Provide to the Engineer written notification and updated Plan sheets for the reinforcement bar lists identifying affected bars.

Mechanical splices of galvanized steel reinforcement shall be in accordance with 709.19.

The following modifications apply to ASTM A767:

5.1 Ensure that steel reinforcing bars to be galvanized are deformed and conform to 709.01, 709.03 or 709.05.

8.1 Random sampling for ODOT’s QA testing requires three 30-inch samples for each bar size delivered to ODOT projects.

8.1.1 Table 2 Minimum Finished Bend Diameters.

| Bar Designation No. | Minimum Bend Diameter (in) |
| --- | --- |
| 3 | 2.25 |
| 4 | 3.00 |
| 5 | 3.75 |
| 6 | 4.50 |
| 7 | 7.00 |
| 8 | 8.00 |
| 9 | 9.50 |
| 10 | 10.75 |
| 11 | 12.00 |
| 14 | 18.25 |
| 18 | 24.00 |

Note: Minimum Bend Diameters (in) in Table 2 supersedes Minimum Bend Diameters 		within Table 509.05-1 Standard Bends.

9.2 All damaged coating shall be repaired in accordance with 711.02.

10.1 Report of test results required.

The following modifications apply to ASTM A1094:

5.1 Ensure that steel reinforcing bars to be galvanized are deformed and conform to 709.01, 709.03 or 709.05.

8.1 Random sampling for ODOT’s QA testing requires three 30-inch samples for each bar size delivered to ODOT projects.

9.1 All damaged coating shall be repaired in accordance with 711.02.

10.1 Report of test results required.

Furnish certified material according to Supplement 1068.