ITEM 422 – DOUBLE CHIP SEAL, AS PER PLAN

The requirement of all language in 422 applies except as modified below:

In Section 422.02 Materials.

Use an CRS-2 emulsified binder conforming to 702.04 for this project.

Remove and replace the first paragraph with ‘For cover aggregate, use crushed gravel meeting 703.05 except the loss, sodium sulfate soundness test, %, maximum: shall be 15. The first course (base course) of the double chip seal shall meet the gradation requirements for #8 size stone. The gradation requirements for the second course (top course) of the double chip seal shall meet the following:

Sieve Size				Total Percent Passing

3/8 inch (9.5 mm)			100

No. 4 (4.75 mm)			70 to 100

No. 8 (2.36 mm)			5 to 50

No. 16	(1.18 mm)			0 to 20

No. 50 (300 um)			0 to 5

In Section 422.07 Binder Application.

For double chip seal, apply the binder at a minimum rate of 0.34 gallon per square yard for the first course (base course) and 0.30 gallon per square yard for the second course (top course).

In Section 422.10 Quality Control

Section “C” is waived.

In Section 422.11 Acceptance.

Section “ E” & “F” is waived.

Section “G” applies to the first course (base course) only. Stone chip applied for the second course (top course) shall fill in all voids.

Project acceptance in 25 to 35 days is waived.