Bridge #3 (GA = 7)

Inspector Comments:

- Overall the bridge is in good condition and warrants a general appraisal of 7.

- The headwall and wings, at the inlet side, are completely covered with map cracks, efflorescence, and a widespread amount of dull sounding concrete. Has some additional isolated areas of spalling around the structures.

  - Inspectors’ recommendation – patch dull sounding and spalled concrete.

- The 72” RCP has some isolated areas of spalling with deteriorating grout at the joints

  - Inspectors’ recommendation – regrout joints and patch spalled concrete.

- The 11’ CMP is in good condition but could benefit from being lined.

- The (6’x9”) arch is in good condition but could benefit from being grouted.

- Will need plenty of fill added for cover over and around the structures.

- Will need to rework the inlet and outlet due to areas of aggradation buildup and streambed degradation to allow for better flow.