Bridge #5 (GA = 8)

Approach: (7)
Sidewalk/Curb – Minor isolated areas of spalling < 2 sq.ft. along the N+S sides
Pavement – Moderate widespread longitudinal/transverse cracks throughout the N+S sides
Slabs – Some minor hairline map cracks with wearing tines throughout the N+S sides
Guardrail – Several moderately damaged section on the NW-SE-SW sides.

Deck: (8)
Expansion Joints – Good condition with minor debris buildup/partial tears between them
Sidewalk/Curb – Moderate widespread hairline map cracks throughout
Parapets – Epoxy coated with several 1/16” vertical cracks throughout the E+W sides
 	*Trees need trimmed along the E side of the bridge – overhanging parapets
Fencing – Good condition
Top of Deck – Some minor hairline map cracks with wearing tines throughout
 	*Existing paint for center line and edge lines is extremely faded
Bottom of Deck – Several minor isolated hairline transverse cracks with efflorescence.

Superstructure: (9)
Beams – 10 beam lines, for 3 spans, appear to be weathering steel with painted ends
 	*Has a few small isolated areas of peeling paint at the end of the beams in span 3
X-Frames – 9 bays, for 3 spans, appear to be weathering steel and in excellent condition
Connection Plates – All appear to be weathering steel and in excellent condition
Bearings – Has a few small isolated areas of chipping paint and minor section loss.

Substructure: (8)
S. wall, rear abutment, is epoxy coated and covered in graffiti with minor isolated areas of vertical hairline cracks. The concrete backwall has some minor hairline cracks.
The concrete slope protection is in excellent condition.
Pier #1 – is epoxy coated and covered in graffiti with minor isolated areas of vertical hairline cracks.
Pier #2 - is epoxy coated and covered in graffiti with minor isolated areas of vertical hairline cracks.
N. wall, forward abutment, is epoxy coated and covered in graffiti with minor isolated areas of vertical hairline cracks. The concrete backwall has some minor hairline cracks.
The concrete slope protection is in excellent condition.

Channel: (N/A)
Has no channel/is a railroad bed.